## Slide 1
Real-Time GW-BSE Investigation on Spin-Valley Exciton Dynamics
Jin Zhao
University of Science and Technology, China (USTC)
VISTA Seminor
Seminor 25
10/14/2021

## Slide 2
Excited Carrier Dynamics in Solar Energy Conversion
Photovoltaics
hot carrier relaxation
electron-hole recombination
interfacial charge transfer
Photocatalysis

## Slide 3
Time-dependent dynamics
Nonadiabatic effects
Different interactions
e-ph coupling
Spin-orbital Coupling
e-h interaction
Challenges for Ab Initio Calculations

## Slide 4
Single Particle Dynamics
Exciton dynamics
Spin Dynamics
Photocatalysis
Photovoltaics
Hefei – Nonadiabatic Molecular Dynamics
(Hefei-NAMD)
valleytronics
optoelectronics
Spintronics
http://staff.ustc.edu.cn/~zhaojin/code.html

## Slide 5
Surface Hopping Combined with TDKS
Nonadiabatic coupling (NAC)
A. Akimov and O. Prezhdo: Pyxaid
Q. Zheng, X. Jiang, et. al. J. Zhao: Hefei-NAMD

## Slide 6
GW + BSE to Describe the Exciton
GW: self-energy take place of exchange correlation potential
Accurate Quasi-particle energies
Bethe-Salpeter Equation (BSE): Screened Coulomb (W) and exchange (v) interaction of electron and hole
Exciton binding energy and wave function

## Slide 7
Exciton Dynamics is Important
Exciton dynamics:
Exciton relaxation
Bright-to-dark transition
Single-to-multi transition
Singlet fission
Exciton annihilation (radiative and nonradiative)
…
10,000 times of GW+BSE calculations are too expensive!

## Slide 8
Realization of GW + Real-Time BSE
BSE Hamiltonian:
Coulomb Interaction:
Exchange Interaction:
Rigid dielectric function during MD
QP energy: Rigid shift from KS energy
10,000 real-time GW + BSE – 1 GW + real-time BSE
from time-dependent Kohn-Sham basis sets
From GW

## Slide 9
Diabatic Representation
TDDFT
Real-time - BSE
Single-particle
two-particle

## Slide 10
Adiabatic Representation
Diagonalize the BSE Hamiltonian to get the exciton basis sets

## Slide 11
Exciton-phonon interaction
Non-adiabatic coupling for exciton
Single particle

## Slide 12
Exciton with Spin

## Slide 13
Exciton dynamics with SOC
Screened coulomb interaciton
Exchange interaction

## Slide 14
TDDFT
Real-time - BSE
Single-particle
two-particle
Many-body interaction：Coulomb and exchange
Exciton-phonon interaction：real-time BSE + molecular dynamics
Spin orbital coupling：adiabatic and diabatic representation
Nonadiabatic: surface hopping
Spin orbital coupling
Realization of GW + Real-Time BSE

## Slide 15
Workflow of Real-Time GW-BSE NAMD

## Slide 16
Fast Intervalley Bright Exciton Scattering in Transition Metal Dichalcogenide
K
K’
K
K’
< 5 ps
Intervalley bright exciton scattering requires the spin flip and momentum transition of both electron and hole
Puzzle：how can such intervalley bright exciton happen within several picoseconds？

## Slide 17
Test of the Dielectric Function Approximation
The dielectric function and GW QP correction almost does not change with the structure

## Slide 18
Time Dependent Quasi-Particle Energies and Optical Band Gap of MoS2
Electron-phonon interaction
Exciton-phonon interaction
A1 mode ~400 cm-1
LA mode ~180 cm-1
A1 mode ~400 cm-1
LA mode ~180 cm-1
+
Time-dependent absorption spectrum

## Slide 19
Exciton Dynamics in MoS2
~1 ps
~1 ps
~40 fs
Bright Exciton transition happens in several ps

## Slide 20
Exchange Interaction Induced Bright Exciton Scattering
Single particle dynamics：e-ph
Exciton dynamics: e-ph + W (e-h Coulomb) + v (e-h exchange) + SOC
Nonadiabatic Coupling Elements：
Bright Exciton transition is induced by e-h exchange interaction

## Slide 21
Single Particle Picture
Spin particle picture: photoexcited hole keeps in K valley

## Slide 22
Ultrafast Charge Transfer at TMD Heterostructure
A1 mode
~400 cm-1
T=83 fs
Q. Zheng, et.al. Nano Lett. 17, 6435-6442 (2017)

## Slide 23
Different Stacking of MoSe2/WSe2
×
×

## Slide 24
Band Structure of MoSe2/WSe2

## Slide 25
Exciton Dynamics at MoSe2/WSe2
100 K
300 K
Electron
Hole
100 K
300 K

## Slide 26
Mechanism of Exciton Dynamics at MoSe2/WSe2
E-ph and SOC
Coulomb Interaction (W)
Exchange Interaction (v)

## Slide 27
Summary
X. Jiang, Q. Zheng, Z. Lan, W. A. Saidi, X. Ren and J. Zhao* Sci. Adv. , 7, eabf3759, (2021)
Xiang Jiang
蒋翔
TDDFT
Real-time - BSE
Single-particle
two-particle
Many-body interaction
Exciton-phonon interaction
Spin orbital coupling
Nonadiabatic effects

## Slide 28
Future work based on GW + rt-BSE NAMD Simulation
Exciton Lifetime
Hot exciton Relaxation
Exciton transition
at interface
via spin valley
bright-to-dark
…
Exciton-Phonon Interaction
Exciton-Polaron interaction
…
Several thousands of exciton energies from GW + rt-BSE NAMD
Machine learning for excited state potential energy surface
Photocatalysis

## Slide 29
Zhenggang Lan
兰峥岗
South China Normal University
Surface hopping
Xingguo Ren
任新国
USTC
GW+BSE
Collaborators
U. Pitt
DFT calculations
Wissam A. Saidi
Jinlong Yang
杨金龙
USTC
Ph.D advisor
Discussion & support
Hrvoje Petek
U. Pitt
Experiments
2011
2013
2015
2016
2017
2019
2020
Acknowledgement
My Group