## Slide 1
Mechanisms and Methodologies for Modelling Excited-State Dynamics in Bare and Hydrated TiO2 Nanoclusters
Miguel Recio-Poo
Departament de Ciència de Materials i Química Física
Institut de Química Teòrica i Computacional (IQTCUB)
Universitat de Barcelona
miguelrecio@ub.edu

## Slide 2
Role of TiO2 in photocatalysis
Titania (TiO2) is a widely used metal oxide in both industrial and environmental applications. Water splitting.
H2 : Clean energy source but against thermodynamics.
Chemical energy
𝚫G0= 237 kJ/mol
Energy
H2O
H2
+ O2
TiO2
Need of external energy. Photocatalytic water splitting. Anatase titania as a potential solution.
Bandgap is too large (3.2 eV). Absorbs only a small fraction of solar spectrum. High recombination rate of electron-hole pairs.

## Slide 3
Electron-hole transportation to the surface
VB
CB
h+
e-
2
1
-
+
-
+
3
-
+
+
-
+
+
4
Bulk
Recombination
(ps-ns)
Surface
recombination
6
H+
H2
5
H2O
O2 + H+
1
2
3
4
5
6
Light irradiation/harvesting
Electron-hole generation
Electron-hole separation
Oxidation reaction
Reduction reaction and H2 generation
H+/H2
H2O/O2
Photoexcitation
(fs-ps)
Surface
reaction
(𝜇s-ms)
(fs-ps)
Key steps in photocatalytic water splitting
4
4
Conduction band
Valence band

## Slide 4
Modelling excited state dynamics
-
+
+
-
+
+
Bulk
Recombination
(ps-ns)
Surface
recombination
TiO₂ is a stable, abundant photocatalyst—but limited by fast electron–hole recombination
Can we tune or extend such recombination times?
Studying excited state: Nonadiabatic molecular dynamics (nanostructuring, hydration,…)

## Slide 5
CP2K: step 1, step 2 (excitations)
Libra: step 2 (overlaps), step 3, step 4
Nonadiabatic Molecular Dynamics workflow
Alexey V. Akimov
A. V. Akimov, J. Comput. Chem. 2016, 37, 1626-1649
STEP 1
STEP 2
STEP 3
STEP 4

## Slide 6
Model Systems: TiO2 Nanoclusters
(TiO2)8(H2O)5
(TiO2)4(H2O)2
(TiO2)4
(TiO2)8
(TiO2)1
(TiO2)2
(TiO2)3
(TiO2)5
(TiO2)7
(TiO2)6
(TiO2)4(H2O)4
(TiO2)8(H2O)2
Part I (JPCC)
Part II (JACS)

## Slide 7
Dependence of excited state dynamics on the hydration degree
S1→S0 (electron-hole recombination)
Benchmark common TD-DFT and NA-MD methodologies
Part I – Hydration and Methodology Assessment
(TiO2)4(H2O)4
(TiO2)8(H2O)5
(TiO2)4(H2O)2
(TiO2)8(H2O)2
(TiO2)4
(TiO2)8
J. Phys. Chem. C 2025, 129 (3), 1806

## Slide 8
Part I - Vibrational and electronic structure
100 to 200 cm-1 -> Ti-O-Ti angle bending
500-1000 cm-1 -> Ti-O stretching
Hydroxyl stretching mode around 4000 cm-1
Classical Dynamics (NanoTiO & FFTiOH)
Ab initio Molecular Dynamics (PBE)
4 ps run (1 ps equilibration + 3 ps production):3000 structures
S0 to S1 state transition
PBE, PBE0 and B3LYP functionals
Hydration increases excitation S1 energies Hybrid functionals mitigate underestimation
S1→S0 transition driven by Ti-O modes
J. Phys. Chem. C 2025, 129 (3), 1806

## Slide 9
Competition between energy difference and isotropy
Hammes-Schiffer-Tully (HST) approach:
Part I - Nonadiabatic Couplings
J. Phys. Chem. C 2025, 129 (3), 1806
HOMO
LUMO
Hydration

## Slide 10
Part I - Nonadiabatic molecular dynamics
NA-MD initialized in S1
15000 trajectories per methodology
J. Phys. Chem. C 2025, 129 (3), 1806
TSH methods:
FSSH, DISH, ID-A, mSDM
Decay evolution fitted to exponential fitting functions
Hydration increases electron-hole recombination rates.
Hybrid functionals and decoherence-corrected methods produce accurate predictions of excited-state dynamics. FFMD vs AIMD agreement.

## Slide 11
Experimentally recorded transient absorption signals
Computations: Time-resolved population-energy spectrograms + DOS
J. Am. Chem. Soc. 2025, 147, 40900–40909
Part II – Relaxation vs recombination
Investigating ultrafast relaxation and recombination in atomically precise (TiO₂)n (n = 1–8) nanoclusters.
Pump: 266 nm, 4.66 eV; Probe: 800 nm
Two lifetimes: τ₁: ultrafast relaxation to S1; τ₂: slower recombination to S0.
Recombination well-captured
by population of S0
Relaxation:

## Slide 12
Slower relaxation to S1 (τ₁) in larger clusters
Recombination to S0 (τ2) depends non-monotonically on the cluster size:
-Slows down when
-Accelerates in larger systems
Part II – Agreement and trends
J. Am. Chem. Soc. 2025, 147, 40900–40909

## Slide 13
Larger NACs between adjacent states are more probable for larger clusters: population spreading among higher-energy states leading to larger τ₁
Part II – Mechanistic explanation
J. Am. Chem. Soc. 2025, 147, 40900–40909
Larger 0-1:3 NACs also accelerate recombination in larger systems.
Larger clusters → greater atomic fluctuations (higher RMSD).

## Slide 14
Conclusions
Influence of water increases excitation energies and generally NACs. Indirect influence: Hydroxyl related modes not coupled to S0→S1 transition. Hydration increases electron-hole recombination rates.
Hybrid functionals and decoherence-corrected methods produce accurate predictions of excited-state dynamics. FFMD vs AIMD agreement.
Two universal pathways identified in (TiO₂)n (n = 1–8): Ultrafast relaxation (τ₁ → S₁) and slower recombination (τ₂ → S₀).
Atomic flexibility and multiconfigurational mixing grow with size → boosts NACs couplings and alters lifetimes. Mechanistic explanation for observerd trends.
Strong experiment–theory agreement → validates Libra + CP2K NA-MD workflow as a predictive tool to analyse excited state dynamics in titania systems.

## Slide 15
Stefan T. Bromley
Ángel Morales García
Francesc Illas
Alexey V. Akimov
5. Conclusions
ESPA Tarragona 2024
Acknowledgments
Mohammad Shakiba
PRE2019-087627
PID2020-115293RJ-I00
PID2021-126076NB-I00
PID2021-127957NB-100
TED2021- 129506B-C22
TED2021-132550B-C22
CEX2021-001202-M
2021-SGR-00079
2021-SGR-00354
GRANT NSF-2045204
Scott Sayres
Chase Rotteger
Hannah Rucker

## Slide 16
(TiO2)4
(TiO2)4(H2O)2
FSSH
DISH
MSDM
ID-A
AIMD + PBE
(TiO2)4(H2O)4
EXTRA
In all cases FSSH yields shorter e--h+recombinationtimes
Faster recombination evolution with increasing degree of hydroxylation

## Slide 17
mSDM method involves a complex description leading to the elimination of coherences and thus to larger decay
Hybrid TD-DFT functionals give rise to faster S1-S0 recombination
Good agreement in final results between ffMD and AIMD!!
(TiO2)8(H2O)2 provides longer times – more convenient for photocatalysis
EXTRA

## Slide 18
Structure–Dynamics Connection
Larger clusters → greater atomic fluctuations (higher RMSD).
EXTRA
The first four columns quantify the degree of configurational mixing: number of determinants contributing to TD-DFT wf.
Other columns show the RMSD of oxygen and titanium atoms
at 100 and 300 K.
Larger atomic fluctuations
cause stronger perturbations of the electronic density resulting in larger NACs.